# corrosim — multiscale corrosion-inhibitor report

Substrate: Fe(110)  |  Medium: 1 M HCl  |  DFT level: B3LYP/6-311++G(d,p) (ddCOSMO:water)  |  Generated 2026-07-14 18:07

The molecules modelled here are screened in silico as representative candidates, not a verified analysis of any real sample. Confirm the actual composition experimentally (e.g. by LC-MS/GC-MS) before drawing firm conclusions.

# 1. Overview

corrosim pipeline

# 2. Summary & ranking

Of the 3 molecules screened, no single lead is robust: pyrazolopyrimidine ethyl ester and pyrazolopyrimidine propanoic acid rank within the method's resolution of one another — the top candidate changes across the 4 descriptor bases (geometry and protonation), so they are reported as a tie rather than ordered. pyrazolopyrimidine propanamide is the robustly weakest candidate, ranked last on every basis. This is a computational screening prediction requiring electrochemical confirmation (see the Method section and caveats).

|  | Pyrazolopyrimidine propanoic acid | Pyrazolopyrimidine ethyl ester | Pyrazolopyrimidine propanamide |
| --- | --- | --- | --- |
| Gap (eV) | 4.655 | 4.659 | 4.665 |
| Hardness η (eV) | 2.327 | 2.33 | 2.332 |
| Softness σ (1/eV) | 0.43 | 0.429 | 0.429 |
| ΔN | 0.166 | 0.168 | 0.171 |
| E_ads (kJ/mol) | -20.42 | -8.81 | -15.55 |
| Fe–O (Å) | 3.85 | 3.95 | 3.85 |
| Score | 1.169 | 0.105 | -1.274 |

| Ranking basis | Top candidate |
| --- | --- |
| force-field geometry, neutral | Pyrazolopyrimidine ethyl ester |
| force-field geometry, pH-weighted | Pyrazolopyrimidine propanoic acid |
| DFT-relaxed geometry, neutral | Pyrazolopyrimidine propanoic acid |
| DFT-relaxed geometry, pH-weighted | Pyrazolopyrimidine propanoic acid |

Lead not robust: the top candidate changes across the 4 bases, so the top group is within method resolution and reported as a tie.

Scored on the HOMO–LUMO gap, hardness and softness of the canonical basis (DFT-relaxed geometry, pH-weighted; z-scored; higher = stronger). The geometry / protonation panels below are a sensitivity check, not separate rankings. E_ads and the Fe–O distance validate the lead, they do not enter the score. Full method: docs/pipeline.md.

# 3. DFT electronic descriptors

Modelled molecules

Frontier-orbital energies vs the metal work function

## 3.1 Frontier-orbital isosurfaces (HOMO / LUMO)

pyrazolopyrimidine propanoic acid HOMO

pyrazolopyrimidine propanamide HOMO

pyrazolopyrimidine ethyl ester HOMO

pyrazolopyrimidine propanoic acid LUMO

pyrazolopyrimidine propanamide LUMO

pyrazolopyrimidine ethyl ester LUMO

Reactivity descriptors

Protonation effect

## 3.2 Full descriptor table (neutral, aqueous)

| Descriptor | Pyrazolopyrimidine propanoic acid | Pyrazolopyrimidine propanamide | Pyrazolopyrimidine ethyl ester |
| --- | --- | --- | --- |
| Formula | C15H14N4O3 | C15H15N5O2 | C17H18N4O3 |
| HOMO (eV) | -6.298 | -6.289 | -6.293 |
| LUMO (eV) | -1.827 | -1.809 | -1.822 |
| Gap ΔE (eV) | 4.471 | 4.48 | 4.471 |
| η hardness (eV) | 2.235 | 2.24 | 2.235 |
| σ softness (1/eV) | 0.447 | 0.446 | 0.447 |
| χ electronegativity (eV) | 4.063 | 4.049 | 4.057 |
| ω electrophilicity (eV) | 3.692 | 3.659 | 3.683 |
| ΔN | 0.169 | 0.172 | 0.171 |
| E_back-donation (eV) | -0.559 | -0.56 | -0.559 |
| TNC | -4.001 | -4.268 | -4.565 |
| E_ads (kJ/mol) | -20.42 | -15.55 | -8.81 |

## 3.3 Geometry refinement (FF vs DFT-optimised)

Force-field vs DFT-optimised geometry

## 3.4 Optimised-geometry descriptors (DFT-relaxed)

| Descriptor | Pyrazolopyrimidine propanoic acid | Pyrazolopyrimidine propanamide | Pyrazolopyrimidine ethyl ester |
| --- | --- | --- | --- |
| Formula | C15H14N4O3 | C15H15N5O2 | C17H18N4O3 |
| HOMO (eV) | -6.347 | -6.334 | -6.337 |
| LUMO (eV) | -1.684 | -1.665 | -1.67 |
| Gap ΔE (eV) | 4.662 | 4.669 | 4.667 |
| η hardness (eV) | 2.331 | 2.335 | 2.333 |
| σ softness (1/eV) | 0.429 | 0.428 | 0.429 |
| χ electronegativity (eV) | 4.015 | 3.999 | 4.003 |
| ω electrophilicity (eV) | 3.458 | 3.426 | 3.434 |
| ΔN | 0.173 | 0.176 | 0.175 |
| E_back-donation (eV) | -0.583 | -0.584 | -0.583 |
| TNC | -3.947 | -4.2 | -4.432 |

Sensitivity: descriptors on the DFT-relaxed geometry (the geometry axis of the ranking ensemble). The headline ranks on the canonical basis; see the Summary.

### Optimised protonated cations (in-acid)

| Descriptor | Pyrazolopyrimidine propanoic acid+H+ | Pyrazolopyrimidine propanamide+H+ | Pyrazolopyrimidine ethyl ester+H+ |
| --- | --- | --- | --- |
| Formula | C15H15N4O3+ | C15H16N5O2+ | C17H19N4O3+ |
| HOMO (eV) | -7.202 | -6.938 | -7.208 |
| LUMO (eV) | -2.798 | -2.412 | -2.786 |
| Gap ΔE (eV) | 4.404 | 4.526 | 4.422 |
| η hardness (eV) | 2.202 | 2.263 | 2.211 |
| σ softness (1/eV) | 0.454 | 0.442 | 0.452 |
| χ electronegativity (eV) | 5.0 | 4.675 | 4.997 |
| ω electrophilicity (eV) | 5.677 | 4.829 | 5.648 |
| ΔN | -0.041 | 0.032 | -0.04 |
| E_back-donation (eV) | -0.551 | -0.566 | -0.553 |
| TNC | -4.329 | -4.458 | -4.903 |

## 3.5 Species in the acidic medium (protonated cation)

| Descriptor | Pyrazolopyrimidine propanoic acid+H+ | Pyrazolopyrimidine propanamide+H+ | Pyrazolopyrimidine ethyl ester+H+ |
| --- | --- | --- | --- |
| Formula | C15H15N4O3+ | C15H16N5O2+ | C17H19N4O3+ |
| HOMO (eV) | -6.978 | -6.736 | -6.965 |
| LUMO (eV) | -3.071 | -2.902 | -3.024 |
| Gap ΔE (eV) | 3.908 | 3.834 | 3.941 |
| η hardness (eV) | 1.954 | 1.917 | 1.97 |
| σ softness (1/eV) | 0.512 | 0.522 | 0.507 |
| χ electronegativity (eV) | 5.025 | 4.819 | 4.994 |
| ω electrophilicity (eV) | 6.46 | 6.056 | 6.329 |
| ΔN | -0.052 | 0.0 | -0.044 |
| E_back-donation (eV) | -0.488 | -0.479 | -0.493 |
| TNC | -4.247 | -4.562 | -4.704 |

Protonated +1 cation descriptors in 1 M HCl; a component of the pH-weighted canonical basis (see the Summary), shown here on its own.

## 3.6 Speciation in 1 M HCl (pH ≈ -0.0)

97% neutral / 3% protonated at this pH — the neutral form dominates. Population-weighted descriptors (the speciation axis of the ranking ensemble; the headline ranks on the canonical basis):

| Descriptor | Pyrazolopyrimidine propanoic acid | Pyrazolopyrimidine propanamide | Pyrazolopyrimidine ethyl ester |
| --- | --- | --- | --- |
| Formula | C15H14N4O3 | C15H15N5O2 | C17H18N4O3 |
| HOMO (eV) | -6.319 | -6.303 | -6.313 |
| LUMO (eV) | -1.866 | -1.842 | -1.859 |
| Gap ΔE (eV) | 4.454 | 4.46 | 4.454 |
| η hardness (eV) | 2.227 | 2.23 | 2.227 |
| σ softness (1/eV) | 0.449 | 0.449 | 0.449 |
| χ electronegativity (eV) | 4.092 | 4.072 | 4.086 |
| ω electrophilicity (eV) | 3.777 | 3.732 | 3.764 |
| ΔN | 0.162 | 0.167 | 0.164 |
| E_back-donation (eV) | -0.557 | -0.558 | -0.557 |
| TNC | -4.008 | -4.278 | -4.569 |

## 3.7 Local reactivity (Fukui)

Pyrazolopyrimidine propanoic acid: O15 (f⁻=0.005), O19 (f⁻=0.000), O20 (f⁻=0.000)

Pyrazolopyrimidine propanamide: O15 (f⁻=0.005), O19 (f⁻=0.000)

Pyrazolopyrimidine ethyl ester: O15 (f⁻=0.005), O19 (f⁻=0.000), O20 (f⁻=0.000)

pyrazolopyrimidine propanoic acid — condensed Fukui

pyrazolopyrimidine propanamide — condensed Fukui

pyrazolopyrimidine ethyl ester — condensed Fukui

## 3.8 Electrostatic-potential (ESP) map

pyrazolopyrimidine propanoic acid — ESP map

pyrazolopyrimidine propanamide — ESP map

pyrazolopyrimidine ethyl ester — ESP map

# 4. Monte Carlo adsorption

pyrazolopyrimidine propanoic acid — best pose

pyrazolopyrimidine propanamide — best pose

pyrazolopyrimidine ethyl ester — best pose

pyrazolopyrimidine propanoic acid — MC annealing

pyrazolopyrimidine propanamide — MC annealing

pyrazolopyrimidine ethyl ester — MC annealing

# 5. Brownian MD (Fe-O RDF)

pyrazolopyrimidine propanoic acid — Fe-O RDF

pyrazolopyrimidine propanamide — Fe-O RDF

pyrazolopyrimidine ethyl ester — Fe-O RDF

# 6. Method & caveats

DFT level: B3LYP/6-311++G(d,p) (ddCOSMO:water). Global descriptors come from the frontier-orbital energies via Koopmans' theorem; ΔN uses the metal work function with η(metal) = 0. The Monte-Carlo and Brownian-MD stages use a classical van-der-Waals adsorption model — a physics-based screening surrogate, not a substitute for periodic DFT or for electrochemical validation. The composite ranking is a heuristic that orders candidates; it does not prove inhibition. Full methodology: docs/pipeline.md; validation record: docs/validation.md.