# corrosim — multiscale corrosion-inhibitor report

Substrate: Fe(110)  |  Medium: 0.5 M H2SO4  |  DFT level: B3LYP/6-31G(d) (ddCOSMO:water)  |  Generated 2026-07-10 18:29

The molecules modelled here are screened in silico as representative candidates, not a verified analysis of any real sample. Confirm the actual composition experimentally (e.g. by LC-MS/GC-MS) before drawing firm conclusions.

# 1. Overview

corrosim pipeline

# 2. Summary & ranking

Of the 1 molecules screened, phytic acid ranks highest on the composite electronic score (+0.00), combining the smallest HOMO–LUMO gap (8.02 eV) with the highest softness — the most readily polarised, electron-donating candidate of the set. It adsorbs flat on Fe in the physisorption regime (E_ads ≈ -11 kJ/mol). This is a computational screening prediction requiring electrochemical confirmation (see the Method section and caveats).

|  | phytic acid |
| --- | --- |
| Gap (eV) | 8.023 ✓ |
| Hardness η (eV) | 4.011 ✓ |
| Softness σ (1/eV) | 0.249 ✓ |
| ΔN | 0.091 |
| E_ads (kJ/mol) | -11.49 ✓ |
| Fe–O (Å) | 3.25 |
| Score | 0.0 ✓ |

Scored on the neutral HOMO–LUMO gap, hardness and softness (z-scored; higher = stronger). E_ads and the Fe–O distance validate the lead, they do not enter the score. Full method: docs/pipeline.md.

# 3. DFT electronic descriptors

Modelled molecules

Frontier-orbital energies vs the metal work function

## 3.1 Frontier-orbital isosurfaces (HOMO / LUMO)

phytic acid HOMO

phytic acid LUMO

Reactivity descriptors

Protonation effect

## 3.2 Full descriptor table (neutral, aqueous)

| Descriptor | phytic acid |
| --- | --- |
| Formula | C6H18O24P6 |
| HOMO (eV) | -8.103 |
| LUMO (eV) | -0.08 |
| Gap ΔE (eV) | 8.023 |
| η hardness (eV) | 4.011 |
| σ softness (1/eV) | 0.249 |
| χ electronegativity (eV) | 4.091 |
| ω electrophilicity (eV) | 2.086 |
| ΔN | 0.091 |
| E_back-donation (eV) | -1.003 |
| TNC | -14.927 |
| E_ads (kJ/mol) | -11.49 |

## 3.3 Local reactivity (Fukui)

phytic acid: O9 (f⁻=0.707), O11 (f⁻=0.099), O10 (f⁻=0.058)

phytic acid — condensed Fukui

## 3.4 Electrostatic-potential (ESP) map

phytic acid — ESP map

# 4. Monte Carlo adsorption

phytic acid — best pose

phytic acid — MC annealing

# 5. Brownian MD (Fe-O RDF)

phytic acid — Fe-O RDF

# 6. Method & caveats

DFT level: B3LYP/6-31G(d) (ddCOSMO:water). Global descriptors come from the frontier-orbital energies via Koopmans' theorem; ΔN uses the metal work function with η(metal) = 0. The Monte-Carlo and Brownian-MD stages use a classical van-der-Waals adsorption model — a physics-based screening surrogate, not a substitute for periodic DFT or for electrochemical validation. The composite ranking is a heuristic that orders candidates; it does not prove inhibition. Full methodology: docs/pipeline.md; validation record: docs/validation.md.